Avalanche Statistics of Dislocation Plasticity
Rohan Tiwari | The Micromechanical Materials Modelling (MiMM) group | IMFD | TU Bergakademie Freiberg

---
Introduction
What is a Dislocation avalanche?
In macroscopic scale, the plastic deformation appears as smooth curve, but in microscopic scale the deformation happens intermittently i.e.,it takes place through strain bursts. This happens due to dislocation avalanche.
Avalanche starts with dislocation accumulation and formation of dislocation bands. The dislocation gets piled up before the bands whose give away causes avalanches(like opening a flood gate)

---
Self-Organized Criticality(SOC):
- Any Slowly driven non-equilibrium systems self-organize themselves in a critical state where anything can happen within well defined statistical laws
- They are Scale-free, intermittent, follows power law distribution and the external driving of the system needs to be much slower than the internal relaxation
- Dislocation avalanches also possess the same character with the power law distribution given by P(A) = A-τ
  where A - Number of bursts
  P(A) - Magnitude of bursts
  τ - 1.6-2.0

---
Measurement of Dislocation avalanches:
- Acoustic emission (AE) is a technique used to measure dislocation avalanches because avalanches generate acoustic waves which can be used to describe its properties
- Ice is used as a model material to study dislocation dynamics from AE because 1) Ice can be easily grown in laboratory 2) Transparency allows to verify AE is not related to micro-cracking 3)Twinning does not occur in ice 4)and AE transducer can be easily coupled by melting/freezing
- One to six piezoelectric transducers of bandwidth 200-750 kHz is attached to the side surface of the cylindrical sample. The dynamic range of the amplitude threshold was set between 30db and 100dB. For each detection above threshold the AE system measures parameters like to , te ,δ and Ao. Acoustic wave form of a dislocation avalanche is shown as follows

---
The wave is recorded is then compared with the acoustic wave having same average duration Ao which provides information about how fast an avalanche damps from initial propagation velocity

---
Dislocation avalanches in single crystal:
Dislocation avalanche in a single Al0.1CoCrFeNi crystal characterized by the interaction between dislocation pileup and dislocation band.

---
Characters of dislocation avalanche in single crystal:
- Avalanche in a single crystal is scale invariant, intermittent and the avalanche size distribution follows a power law
- The general form of the avalanche strain distribution in a single crystal is given by P(s) = Cs-τ exp[-(s/so)2]
  where C is normalization constant and S0 is the characteristic strain of the largest avalanches
- The avalanche size distribution is unaffected by the internal variables like material and crystal structure and also by the applied stress

---
 Strain avalanche in sub-micron plasticity of FCC metals:
- Since there is not much slip planes in sub-micron level the yield strength and hardening depends on the size of the sample chosen
- Stress-strain relationship is characterized by 1)high and stochastic flow stress 2) post yield stress has strain oscillations accompanied with dislocation avalanches
- When nickel nano-pillars are studied using 3-D dislocation dynamics it showed the creation and destruction of dipolar loops
- When the stress reaches first yield point the dipolar loops interact with boundary leaving behind the pillar trail of debris and the stress starts to rise in order to keep up with the applied strain
- When stress reaches critical value the debris become the fresh source of dislocation and the cycle of dislocation starvation and production happens continuously leading to strain oscillations

---
Stress-strain curve of sub-micron plasticity in FCC-metals
From these observations, it is found that the strain avalanching of FCC crystal is dependent on the dislocation density and the presence of dipolar loop. But these parameters are found to have no effect on the universal size distribution of avalanches.

---
Effect of temperature on avalanches:
- To find the effect of temperature on the behaviour of dislocation avalanches uniaxial compression creep test are carried out on ice crystal from -20 to -30C
- Even thought the temperature affects the behaviour of individual dislocations like the velocity, relaxation time etc., it does not affect the size distribution of the avalanches
Avalanche size distribution in ice crystal at different temperatures

---
Dislocation avalanches in Polycrystals:
- In polycrystals, the propagation of dislocation avalanches is hindered by the presence of Grain boundaries(GBs)
- The avalanche size distribution of polycrystals differ from single crystals in two ways 1)Power law exponent is smaller 2) cut-off of power law scaling at larger amplitudes
Avalanche size distribution of polycrystals compared with single crystals

---
- The interaction of dislocations and GBs creates sudden internal stress which breakdown one of the main necessary condition for SOC i.e., an external driving rate much smaller than internal relaxation process
- As a consequence the system is forced to relax internal stress through a single large aftershock into neigbouring grain which then triggers the secondary avalanches in the neighbouring grain
- This is the main reason for strain hardening in polycrystalline materials during plastic deformation and during the transient creep the level of hardening was found to increase with decreasing grain size
- Therefore the presence of grain boundaries affect the scale-free,intermittent, close-to-critical dynamics of the propagation of avalanche size distribution